## Slide 1
Paul M. Grant www.w2agz.com
Aging IBM Pensioner
IBM Almaden Research Center
650 Harry Road
San Jose, CA
ARC Auditorium
10:30AM – 11:30AM
Friday, 6 May 2011
To
Electric Power
From Electrons Paired
…And… Back
Again
?
-- A Personal Journey in Superconductivity --
-- IBM, EPRI, and Beyond --

## Slide 2
A DFT (LDA+U) Study of the Electronic Properties of Square-Planar Coordinated
Copper Monoxide Structures
… And Now for Something Completely Different …
Back to the Future…
My IBM SJRL Day Job of the 60s and 70s…
Electronic Structure Calculations
Notes: 2
2
2

## Slide 3
Transition Metal Oxides
“Should be Metals, But Aren’t” (Charge Transfer Insulators, Instead)
After Imada, et al, RMP 70, 1039 (1998)‏
Mott
Hubbard
Anderson
Brooks
Feinlieb
RPA Doesn’t Work!
Notes: 3

## Slide 4
TM
O
Cubic Rocksalt TMO
a = b = c
Cubic Rocksalt TMOs
Direct and Reciprocal Lattices

## Slide 5: Cubic Rocksalt Divalent TMOs
TMO 3d Config Properties
MnO 5 MH-CTI (5.6)
FeO 6 MH-CTI (5.9)
CoO 7 MH-CTI (6.3)
NiO 8 MH-CTI (6.5)
CuO 9
XX Doesn't Exist!
See Imada, Fujimore, Tokura, RPM 70 (1988)‏
Why Not?
Notes: 5

## Slide 6
Tenorite (Monoclinic CuO)‏
Cu
O
What God wants…just ask her!
Notes: 6
6

## Slide 7
DFT & (LDA + U)‏
Implemented in LMTO by Anisimov, et al, JPCM 2, 3973 (1990)‏
  Applied to NiO, MnO, FeO, CoO and La2CuO4
Plane-Wave Pseudopotential Implementation by Cococcioni and de Gironcoli, PRB 71, 035105 (2005)‏
  Applied to FeO and NiO
  Download open-source package from http://www.pwscf.org
Can Application of DFT (LDA+U) Help Unravel the Cubic Rocksalt CuO Enigma?
…Let’s see…
Notes: 7

## Slide 8: Proxy Structures A New Materials Science Discipline
You want to understand the basic physics of some given system…(e.g., HTSCs)
So try to synthesize a simple proxy…(e.g., rocksalt CuO)
But “Mother Nature” won’t “agree.” (She’s a woman!)
However, you can build it in a computer and perform various “ab initio” experiments.
And from such, numerically calculate “observables,” e.g., “response functions.”
Try it out…it’s lots of fun! And perhaps you’ll discover something as well!

## Slide 9
Tools
QUANTUM-ESPRESSO Suite of Codes
  DFT (LDA+U) plus electron-phonon
  Graphics by Tone Kolalj (XCrysDen)
  www.quantum-espresso.org
“Dial-in” Parameters
  G2 = 40 Ry ρ = 320 Ry
  Convergence ≤ 10-6 Ry
  “Smearing” = Methfessel-Paxton
  Psuedopotentials: Ultrasoft, XC = Perdew-Zunger Cu: 3d94s2 O: 2s22p4
  Hardware
  3.33 GHz Intel Core i7 – 12 GB+ (Gaming Box – Home Built)
  Software Linux Kubuntu
Viva Italia!

## Slide 10
Rocksalt CuO Band Widths U = 0 eV
Note Degeneracies! 8 Cu3d – O2p Bands
Notes: 10

## Slide 11
Rocksalt CuO Fermiology (U = 0 eV)
(8 Bands Combined)
Note (Near) Degeneracies!
Jahn-Teller Unstable?
Alex M?
(maybe you were on the right track, after all!)
Notes: 11

## Slide 12
Non-Magnetic (U = 0) Cubic Rocksalt CuO -- Electron-Phonon Properties --
λ ~ 0.6 – 0.7
Consistent with other non-magnetic “HTSCs”
α2F(ω)
σ = 0.04
 | TC (K) | λ | μ*
K3C60 | 16.3 | 0.51 | -
Rb3C60 | 30.5 | 0.61 | -
Cs3C60 | 47.4 | 0.72 | -
Notes: 12
12

## Slide 13: Are There Phonons w/ High-Tc in YBCO?
Fig. 38: Pintschovius and Reichardt, in Furrer, ISBN 0-7923-5226-2

## Slide 14: Yes -- They’re There!
Pyka, et al., PRL 70, 1457, (1993)
Harashima, et al., Physica C263, 257 (1996)

## Slide 15
Macfarlane, Rosen, Seki, SSC 63, 831 (1987)
Raman Spectroscopy of YBCO

## Slide 17: Proto-TMO AF-II Rocksalt Unit Cell
[111]
Applies to:
MnO
FeO
CoO
NiO
CuO ?

## Slide 18: Proto-TMO AF-II Rocksalt
[-1-1-1]

## Slide 19
The Answer(s) !
TMO Asymmetric Type II
af-CuO Cell
LDA+U Calcs
Grant, IOP-CS 129 (2008) 102042 (Click Here)
Tetragonal Distortion
Siemons, et al, PRB 79 (2009) 195122 (Click Here)

## Slide 21
References
“Electronic Properties of Rocksalt Copper Monoxide,”
APS MAR09-2008-006217, P. M. Grant, Pittsburgh (2009)

## Slide 22
“Non-Fermi Liquid” ‘Nematic Fermi Fluids’
“Whatever!”
“Fermi Liquid” “Dilute Triplon Gas”
“Whatever!”
“SDW” “NEEL” “A-F”
“Whatever!”
T
g
g* “QCP”
“Insulator”
“Conductor”
ρlocal
The Great Quantum Conundrum

## Slide 23
“Real Metal” “Fermi Liquid”
“Funny Metal” “Pseudogap” “Fond AF Memories”
“SDW” “NEEL” “A-F”
Superconductivity
T
g
g* “QCP”
“Insulator”
“Conductor”
ρlocal
“Funny Metal” “Pseudogap” “Fond AF Memories”
The Colossal Quantum Conundrum

## Slide 24
U = 0
n = 0.00
n = +0.15
n = -0.15
Hubbard (eV)
“Doping” (-e/CuO)

## Slide 25
U = 3
n = 0.00
Hubbard (eV)
“Doping” (-e/CuO)
n = +0.15
n = -0.15

## Slide 26
U = 6
n = 0.00
n = +0.15
n = -0.15
Hubbard (eV)
“Doping” (-e/CuO)

## Slide 27
n
U
0
3
6
0.00
+0.15
-0.15

## Slide 28
“Real Metal” “Fermi Liquid”
“Funny Metal” “Pseudogap” “Fond AF Memories”
Superconductivity
“SDW” “NEEL” “A-F”
T
g
g*
“Insulator”
“Conductor”
“Funny Metal” “Pseudogap” “Fond AF Memories”
The Colossal Quantum Conundrum
U~U0 exp(-α g), g < g*; 0, g > g*
Somewhere in here there has to be “BCS-like” pairing!
U = 6
U = 0
U = 3

## Slide 29
Shakes or Spins or Both?
Are They Copacetic, Competitive…or…
…just another Conundrum?
What formalism is the HTSC analogy to Migdal-Eliashberg-McMillan?
Original Strong Coupling, Eliashberg (JETP, 1960), McMillan (PR, 1968)
Generalized Linhard Response Function (RPA + fluctuations) Hu and O’Connell (PRB 1989)
Dielectric Response Function Kirznits, Maximov, Khomskii (JLTP 1972)
(In other words, how do I calculate the value of the BCS gap?)

## Slide 30: McMillan Strong Coupling
(Computationally implemented by Wierzbowska, et al., cond-mat/0504077, 2006)
What’s the HTSC equivalent?

## Slide 31: Generalized Linhard Function
HO (1989)
“Fluctuations?”
“Empirical?”

## Slide 32: Dielectric Response Function
KMK (1972)
In principle, KMK can calculate the BCS gap for general “bosonic” fields, be they phonons, magnons, spin-ons, excitons, plasmons…or morons!

## Slide 33: Bottom Line
Can studying CuO proxies with DFT
+ LDA+U
+ phonons
+ spins
provide insight into the origins of High-TC?
I say “Yes,” but…
Size Matters…
…and I need a…
BIGGER COMPUTER!

## Slide 34: Other CuO Proxy Structures
- Studies in Progress -

## Slide 35
Films & Tubes
a = b = 3.905 Å c = 6 x 3.905 = 23.43 Å
5.226 Å
2.00 Å
2 CuO segments per quadrant
16 Å between tubes

## Slide 36
Films & Tubes Zones

## Slide 37
Films & Tubes States
Landauer – Buettiger?

## Slide 38
-- OK…Enough Already !
-- That’s all for now !
-- But Stayed Tuned…