## Slide 1
Setup

## Slide 2
Challenges Confronting High Temperature Superconducting Materials:
From Nanoscale Theories
to
Exascale Energy Applications
Aging IBM Pensioner
Research Supported by IBM Retirement Fund
2014 MRS Spring Meeting
Symposium T
Marriott Marquis
21-25 April 2014, San Francisco, CA
Paper T7.03
Yerba Buena Level, Salon 15
2:30 PM
Wednesday, 23 April 2014
Paul M. Grant
W2AGZ Technologies
EPRI Science Fellow (Retired)
IBM Research Staff Member/Manager (Emeritus)
Notes: 2
2
2

## Slide 3
HTSC Symposium, MRS Spring Meeting, Anaheim, 23-24 April 1987
“The Altamont of Materials”

## Slide 4
It is now 27 years to the day after “Altamont,” yet two major issues remain unresolved:
“The Nanoscale:”
How does HTSC even occur? We know it’s BCS, so what’s the “pairing glue?”
“The Exascale:”
Despite more than 20 years of very successful HTSC wire development possessing outstanding critical state properties, and its use in equally outstanding and successful power application demonstrations in the US, Japan, China, Korea, Germany, Russia..., there remains no significant deployment of such technology by either government agencies or investor-owned utilities.
How come?

## Slide 5
“Real Metal” “Fermi Liquid”
“Funny Metal” “Pseudogap” “Fond AF Memories”
Superconductivity
“SDW” “NEEL” “A-F”
T
g
g*
“Insulator”
“Conductor”
“Funny Metal” “Pseudogap” “Fond AF Memories”
The Colossal Quantum Conundrum
U~U0 exp(-α g), g < g*; 0, g > g*
Somewhere in here there has to be “BCS-like” pairing!
U = 6
U = 0
U = 3
Our Proxy HTSC!
“Undoped Rocksalt
Copper Monoxide”
NB2: For U < 6 eV, it’s a metal!
NB1: These BZ’s & FS’s reflect an af-ordered, 2x periodic primitive unit cell.

## Slide 6
“Put-on !”
IOW, What’s theFermion-Boson Interaction That Leads to HTSC?
Notes: 6

## Slide 7: The Pairing Glue
“Alex says it’s phonons”
OK, OK...J-T polarons and/or bipolarons (after Chakravarty/Hoest)
Could he be right after all?

## Slide 8
Macfarlane, Rosen, Seki, SSC 63, 831 (1987)
(These data were taken in early March, 1987, a week before “Woodstock”)
Raman Spectroscopy of YBCO
Hey! Maybe, they’re there!

## Slide 9: More Phonon Phootprints!
Pyka, et al., PRL 70, 1457, (1993)
Harashima, et al., Physica C263, 257 (1996)

## Slide 10
...and More!

## Slide 11
Ledbetter, Physica C 235, 1325 (1994)
Finally, TC scales (roughly) with D !
Nota Bene!
“S” denotes Ca, Sr, Ba

## Slide 12: What Can DFT(LDA+U) Along With Eliashberg-McMillan-Allen-Dynes (EMAD) Formalism Tell Us About e-p Mediated Pairing in the Copper Oxide Perovskites?
Assume the simplest and highest symmetry possible Cu-monoxide to model (e.g. cubic or tetragonal rocksalt CuO...see Grant (Proc IOP (2008) and Siemons, et al., PRB (2009)).
Apply the Quantum-Espresso DFT Package to calculate the eigenspectrum and e-p coupling for these proxy structures, followed by application of EMAD to estimate Tc (Grant, Proc. MRS, to appear).
Perform the above for both hole and electron doping levels 0.15|e|/CuO under the assumption these levels of carrier densities effectively screen Hubbard U (see “Quantum Conundrum”)

## Slide 13: So let’s do it and “compute” what happens!
≈ 43 °K
≈ 25 °K
Assumptions: ≈ 440 K, * ≈ 0.01, a = 3.06 Å, c/a = 1.3 (nmTet cell)
q = 0.15 |e|/CuO (holes)
q = -0.15 |e|/CuO (electrons)
 = 1.2
 = 0.7

## Slide 14: OK...What’s Next (Materials-Wise)?
Force-epi 10 monolayers of tet-CuO
  Overlay with 2 monolayers of Li as “neighborhood” dopant...look for SC
  “Topological Metal?” 
Look for explicit “phonon-spinon” coupling:
  “Paramagnetic Dispersion Measurements at 77.3 K,” C. Starr (MIT). Examines the coupling between spins and phonons in transition metal carbonates and hydrates.
  Published in Phys. Rev. 60, 241 (1941!)
  Have such studies been done on the copper oxide perovskites? If not, why not?
Apparently no DFT(LDA+U) tools yet exist to calculate electron-phonon  in the presence of a finite Hubbard U...why not?

## Slide 15: Now for something slightly bigger... by 1019 (Exascale!)
SuperCity
SuperSuburb
SuperGrid
SuperTrain

## Slide 16: HTSC SuperCables: Past, Present, and...Future?
EPRI SCDC
100 kV, 100 kA, 10 GW
Sumitomo 66 kV 3-in-1
Furakawa, 275 kV, 3 kA
St. Petersburg, Russia
~ 1997
~ 2013

## Slide 17: Required Reading! (Thanks to Steve Eckroad, EPRI)
Two EPRI Reports (available free from epri.com or w2agz.com)
  (2012) Superconducting Power Equipment; Technology Watch 2012 (1024190)
  (2013) SIU: Superconductivity for PDA (03002001)
Bottom Lines:
  Work continues on wire improvement and power application demonstration, although not at the pace of a decade ago.
  HTSC materials performance and costs have matured.
  What’s needed is a strong business case for HTSC power applications.
  Does there exist a “compelling need,” now or in the next decade, to effect a major and continuing deployment of HTSC in the electricity enterprise?

## Slide 18: Pacific Intertie
HVDC, +/- 500 kV, 3.1 kA, 3.1 GW
1,362 km
~50% of LA Power Consumption
T&D Losses ~ 10%
Tear down the PI and replace with HTSC underground cables to capture this saving?
Ain’t gonna happen, baby!
Not a “compelling need!”
Even should the cost of the wire be zero!

## Slide 19: However, do we have a “compelling new opportunity?”
P.M. Grant, EPRI, 1998

## Slide 20: Why not make dual-use of emerging gas pipeline rights-of-way to transport electricity via HTSC cables?
Natural Gas & Electricity!
Chart: 
| Coal | Natural Gas | Nuclear | Hydroelectric | Renewables | Other
2012 | 0.38407 | 0.31155 | 0.19475 | 0.070003 | 0.055384 | 0.010612
2012 USA Electricity Generation by Primary Fuel Source
Wow!
“Fraternal Twins,”
Smart Grid News
16 April 2013

## Slide 21: Not exactly a new idea! (Terry Boston, TVA VP, 2001)

## Slide 22: Does “Keystone XL” Provide a “Compelling Opportunity” to “Raise Our Fraternal Twins?”
Let’s encourage DOE to enlist EPRI, GTI, EIPC, INGAA,...in a collaboration to conduct an “engineering economy” study focused on the dual-use ROW concept.

## Slide 23
...and in the long term...
Electricity Conversion Assumptions
Wellhead Power Capacity | 18 GW (HHV)
Fraction Making Electricity | 33%
Thermal Power Consumed | 6 GW (HHV)
Left to Transmit as LNG | 12 GW (HHV)
CCGT Efficiency | 60%
Electricity Output | 3.6 GW (+/- 18 kV, 100 kA)
“Cryodelivery Systems for the Cotransmission of Chemical and Electric Power,”
P.M. Grant, AIP Conf. Proc. 823, 291 (2006).

## Slide 24
o Wroclaw
The Wola Obszańska (Lublin) gas field in Poland/Ukraine was discovered in 1989. It began production in 1992 and produces natural gas. The total proven reserves of the Wola Obszańska gas field are around 37 billion cubic feet (1×109m³). “Dual-Pipe” to Berlin?
Let’s Not Forget Europe!

## Slide 25: Back to the Future (of Nanoscale!)
The Grand Challenge of Materials Science: Can we make a room temperature superconductor?
  Bill Little says “yes” (1963)...simply surround a 1D metal chain with polarizable molecules and use “excitons” as the “pairing boson.”
  Problem: Periodic 1D metals are unstable and want to became insulators (dimerization).
Solution:
  Create a 1D Fibonacci (quasiperiodic) chain of “metal” atoms that resists CDW and dimerization “gapping” instabilies on a suitable “polarizable” substrate.
  How? “Decorate” a dislocation line on the [100] surface of STO, SRO, Si...

## Slide 26: A Fibonacci “Dislocation Line”
tan  = 1/ ;  = (1 + 5)/2 = 1.618… ;  = 31.717…°
STO ?
SRO !
Al
Al
Al
Al
Al
Al
Al
L = 4.058 Å (fcc edge) s = 2.869 Å (fcc diag)
From P.M. Grant, APS March Meeting, Portland, OR (2010)

## Slide 27
Does the Hold the Key to Room Temperature Superconductivity?
50th Anniversary of Physics Today, May 1998

## Slide 28: Lessons from “Four Altamont Philosophers”
...for materials scientists under 50...

## Slide 29: “You can’t always get what you want…”

## Slide 30: “…you get what you need!”