## Slide 1: Setup

## Slide 2
A DFT Study of Tetragonal Rocksalt Proxy Copper Monochalcogenide Structures:
-- Implications for Possible High-Tc Superconductivity --
Paul M. Grant
W2AGZ Technologies
Robert H. Hammond
Stanford University
AFOSR Superconductivity
Program Review 2014
18 August 2014 Arlington, VA
A Sheynem Dank, Biz Hundert,
Reb Harold!

## Slide 3: – Our Computational Tool Box –
DFT + Hubbard U
  Quantum Espresso
    Bands, Fermiologies, States (DOS), Phonons
Graphics
  Xcrysden, XMGRACE
    Bandwidths, Fermi Surfaces, Projected DOS
Modeling
  Neel Temperatures a la Van Vleck/Anderson/Hubbard
  Superconductivity via Eliashberg/McMillan

## Slide 4
“Configuration/Coordination Space”
Relative Ground
State
Energies
Tennorite
The Various Flavors of Copper “Monoxide”
“1-2-3”
tet-rs-CuO
Siemons, et al. (2009)
Grant (2008)
Franchini Group (2011)
Cococcioni Group (2011)
Can we compute/synthesize
the S, Se, Te analogues
...and what would be their physical properties wrt magnetism and superconductivity?

## Slide 5: Rocksalt af-CuX Crystallography
nm-Translational Unit Cell
Cu (Blue)
X (Red)
af-Primitive Cell
X (Red)
Cu (Bronze, Green)
Note: The af-”translationally asymmetric unit”
contains
two Cu ions to correctly represent the doubly-periodic spin up/down ordering
“U”
Brillouin
Zone

## Slide 6
CuO (a ≈ 4.1 Å)
CuS (a ≈ 4.7 Å)
CuX (Cubic, Equilibrium Lattice Constant(s))
CuSe (a ≈ 5.0 Å)
CuTe (a ≈ 5.3 Å)

## Slide 7
What Does Experiment Say About Rocksalt CuO?
It’s Tetragonal(!) for 4-6 monolayers forced-epi grown on STO yielding a film with lattice constants a = b = 3.905 Å, and c/a ≈ 1.3, representing a 5% basal-plane contraction down from pure cubic having a = b = c = 4.1 Å. (Siemons, et al, PRB 79, 195122 (2009))
EF
E (eV)‏
N(E) (eV-1)‏
He I UPS Spectrum
W. Siemons (PhD Thesis, Stanford)‏
See Fig. 9 in Grant, IOP-CS 129, 012042 (2008)

## Slide 8
CuX (Tetragonal)
CuO (a = b ≈ 3.9 Å; c/a ≈ 1.3)
CuS (a = b ≈ 4.5 Å; c/a ≈ 1.1)
CuSe (a = b ≈ 4.75 Å; c/a ≈ 1.1)
CuTe (a = b ≈ 5.05 Å; c/a ≈ 1.1)
(Assuming a 5% contraction of the a, b lattice constants a la CuO on STO)

## Slide 9
CuO
CuS
CuSe
CuTe
Cubic CuX
U= 0

## Slide 10
Cubic CuX
U= 6
CuO
CuS
CuSe
CuTe

## Slide 11
Tet-rs CuX
U= 0
CuO
CuS
CuSe
CuTe

## Slide 12
Tet-rs CuX
U= 6
CuO
CuS
CuSe
CuTe

## Slide 13
CuO
CuS
CuSe
CuTe
All Tet
All U=6

## Slide 14
CuS
Bandwidths
All Tet. All U=6
CuO
CuSe
CuTe

## Slide 15: Van Vleck /Anderson/Hubbard Model of Neél Temperature
Take the definition of “Exchange Energy” from Anderson (1959):
where tij is the transfer integral from the spin states on one TM ion, directly to a neighbor, or through an intervening anion, and U is the on-site Hubbard coulomb repulsion potential, e.g.,
Now, “plug into” Van Vleck (1938-42), within the “molecular field approximation,” to get TN:
Here S is the net cationic spin and kB the Boltzmann constant (8.61733•10-5 eV/°K).
The “transfer integrals” are given by,
where the ϕ’s are the “spin carrying” orbitals and H a “tight-binding-like Hamiltonian.”

## Slide 16: Néel Temperature vs. TMO
TN (K)

Tenorite
Tet-CuO
From Kittel
?

## Slide 17
a = b = 3.9 Å
c/a = 1.3
S = 0.5
U = 6.0 eV
Tet-rs-CuO
Bandwidths, wi,j (eV)
2.02
2.04
1.47
1.73
(1)
(2)
(3)
(4)
°K
(1) 494
(2) 501
(3) 261
(4) 360
°K
1+2 = 994
2+3 = 762
1+2+3 = 1255
?

## Slide 18: Néel Temperature vs. TMO
TN (K)

Tenorite
Tet-CuO (1+2)
From Kittel

Tet-CuO (2+3)
?

## Slide 19
a = b = 4.5 Å
c/a = 1.1
S = 0.5
U = 6.0 eV
Tet-rs-CuS
Bandwidths, wi,j (eV)
2.92
3.58
3.27
3.70
3.45
(1)
(2)
(3)
(4)
(5)
°K
(1) 1030
(2) 1551
(3) 1292
1659
1436
Such high values of TN most
likely reflect a breakdown of
the simple tight-binding VVAH model when “X” > “O” in CuX

## Slide 20: Superconductivity(?) Phonons(?) Eliashberg-McMillan
Need to compute
!

## Slide 21: e-p Interaction in the DFT/LDA Formalism

## Slide 22
“Real Metal” “Fermi Liquid”
“Funny Metal” “Pseudogap” “Fond AF Memories”
Superconductivity
“SDW” “NEEL” “A-F”
T
g
g*
“Insulator”
“Conductor”
“Funny Metal” “Pseudogap” “Fond AF Memories”
The Colossal Quantum Conundrum
U~U0 {1 - (g/g*)2}1/2
Somewhere in here there has to be “BCS-like” pairing!
Perhaps phonon-mediated?
U = 6
U = 0
U = 3

## Slide 23
Well, how about the “U = 0, Fermi Liquid” limit
for doped proxy tet-CuO?
U
K
K
Y
Z
G
eV

## Slide 24: So let’s do it and “compute” what happens!
q = 0.15 |e|/CuO (holes)
q = -0.15 |e|/CuO (electrons)
≈ 43 °K
≈ 25 °K
Apply DFT to obtain between electrons and phonons, followed by application of the Eliashberg-McMillan-Allen-Dynes formalism to find Tc:

## Slide 25: Whither Superconductivity in the TM Mono-VI’s?
CuO (Tet a=3.9 Å, c/a=1.3, U=0, q=0.15 |e|/CuO)
CuS (Cub a=4.7 Å, c/a=1.0, U=0, Undoped)
Note:
, N(Ef) ~ 0.5 that for CuO. Tc = ?

## Slide 26: Can We Really Make Any of This Stuff?
Forced-epitaxial thin film growth is obvious choice (as it was with tet-CuO. Substrate selection likely limited, but here are possible choices:
  CuS (4.7 Å) Rocksalt ZnO (4.580 Å, ~3% compression)
  Rutile TiO2 (4.591 Å, ~2.5% compression)
  CuSe (5.0 Å) Hex Al2O3 (4.748 Å, ~5% compression)
  CuTe (5 .3 Å) Cubic ZrO2 (5.147 Å, ~5.3% compression)
  YSZ (5.13 – 5.23 Å, ~3.5% compression max)
  CaF (5.46 Å, ~3% expansion)
Methodologies
MBE - PLD:
  Use appropriate sintered sample source.
  Empirically determine optimum substrate temperature and argon pressure.
  Characterize growth and structure via in-situ “high pressure compatible” RHEED, XPS, UPS, LEED.
External characterization, depending on stability in air:
  4-probe transport.
  UV-Vis optical transmission and reflectivity.

## Slide 27: “An Ideal Lab”

## Slide 28: The Bottom Line(s)
For X = S, Se and Te, neither a finite U or a “5% basal” tetragonal distortion has much effect on their respective CuX Fermiologies, and likely transport/magnetic properties dependent thereon.
However, the respective Fermi surfaces ...may...may... contain nesting topologies promoting itinerant antiferromagnetism a la Cr, but, unlike Cr, here for X = S, Se, Te, the DOS at Ef is dominated by p-like chalcogenide overlap.
Future homework for proxy structure modelling, suggested by preliminary results on “doped” tet-CuO: Let’s look for electron-phonon mediated superconductivity!
But ...most importantly... experiment always rules. Our fundamental computational finding is that equilibrium rocksalt CuS, CuSe and CuTe structures can in principle exist ...so let’s try to make and dope them and henceforth measure their properties!
Finally, there is something quite special about the Cu-O bond in square-planar symmetry!
...but we knew that already... in 1986 B & M told us so!

## Slide 29: Addenda Forward -- What’s the Path to Higher Tc? --
All known HTSCs are “strong coupled BCS” systems...exclusive of “whatever boson” may be involved.
  Beasley/Gurevich have shown strong coupling yielding Tc’s ~ 190 K will lead to ’s < atomic radius.
  Not likely!
  So what’s the escape route?
Weak BCS coupling employing higher energy bosonic glue...e.g., “excitons,” aka Bill Little’s model.

## Slide 30: Phononic, Plasmonic, or...Excitonic,?
“Organic Perovskites”
Mitzi (1999)

## Slide 31: Back to the Future...PRB 1976
This dispersion relation is at the heart of the “Little Model”
Kirshnitz, Maximov & Khomskii (KMK)
Assume for a given model we compute the ground state eigenstates via DFT...we then need to code KMK and apply to estimate Tc...
Let’s do it, People!

## Slide 32
tan  = 1/ ;  = (1 + 5)/2 = 1.618… ;  = 31.717…°
A Fibonacci “Dislocation Line”
“Scratch” along the 100 surface of single crystal, say Si, and then “decorate” with a line of, say Al atoms. Then use DFT + KMK to test “Bill’s idea.”

## Slide 33: The Future? Physics Today, November 1998
700 K !
May, 2028
NB! The plot of this story is fiction...
But the Science is not!