## Slide 1: Setup

## Slide 2
A DFT Study of Electron-Phonon Coupling in
Proxy CuX (X = S, Se, Te) Structures and Its Relationship
to Possible Manifestation of Superconductivity
Paul M. Grant
W2AGZ Technologies
Robert H. Hammond
Stanford University
Session Q11
Chalcogenide Superconductors
2:30 PM – 4:54 PM, Wednesday, 4 March
Paper 11
4:06 PM – 4:18 PM
Room 007B

## Slide 3: – Our Computational Tool Box –
DFT + Hubbard U
  Quantum Espresso
    Fermiologies, States (DOS), Phonons, e-p “Lambda”
Graphics
  Xcrysden, XMGRACE
    Fermi Surfaces, Projected DOS
Modeling
  Debye Temperatures a la Gibbs2 Package
    Thanks to Alberto Otero-de-la-Rosa, http://azufre.quimica.uniovi.es/src/gibbs2/gibbs2.pdf
  Then Superconductivity via Eliashberg/McMillan!

## Slide 4
“Configuration/Coordination Space”
Relative Ground
State
Energies
Tennorite
The Various Flavors of Copper “Monoxide”
“1-2-3”
tet-rs-CuO
Siemons, et al. (2009)
Grant (2008)
Franchini Group (2011)
Cococcioni Group (2011)
Can we compute/synthesize
the S, Se, Te analogues
...and what would be their physical properties wrt magnetism and superconductivity?
Magnetic properties revealed at APS MM Denver 2014. Now superconductivity!

## Slide 5
CuO
Ground State Energies via Gibbs2: CuO & CuS
CuS
Min GSE at a0 = 4.13 Å
(Cubic)
Cubic
CuO (Cubic)
D = 693 K
Min GSE at a0 = 3.9 Å, c/a = 1.15
Tetragonal
CuO (Tet)
D = 733 K
Min GSE at a0 = 4.75 Å
CuS (Cubic)
D = 525 K
Min GSE at a0 = 4.5 Å, c/a = 1.12
CuS(Tet)
D = 780 K

## Slide 6
CuSe
CuTe
Ground State Energies via Gibbs2: CuSe & CuTe
Min GSE at a0 = 5.0 Å
Cubic
CuSe (Cubic)
D = 409 K
Min GSE at a0 = 5.34 Å
CuTe (Cubic)
D = 327 K
Min GSE at a0 = 4.75 Å, c/a = 1.1
Tetragonal
CuTe (Tet)
D = 622 K
Min GSE at a0 = 5.05 Å, c/a = 1.1
CuTe (Tet)
D = 489 K

## Slide 7: Superconductivity and Phonons BCS via Eliashberg-McMillan
To get , need to compute
!
NB! The “double deltas” will be approximated by two Gaussians of width “sigma ()” whose numerical convergence is governed by imposed precision limits and basis set symmetry. Con Quidado!

## Slide 8: Eliashberg-McMillan-Allen-Dynes
Let’s Go!

## Slide 9
CuSe
TC
D = 409 K; * = 0.0
Cubic
TC(max) ~ 17 K
Tetragonal
TC(max) ~ 36 K
D = 623 K; * = 0.0

## Slide 10
CuTe
TC
D = 327 K; * = 0.0
Cubic
TC(max) ~ 4.2 K
Tetragonal
TC(max) ~ 45 K
D = 490 K; * = 0.0

## Slide 11
CuS
TC
D = 525 K; * = 0.0
Cubic
TC(max) ~ 28 K
Tetragonal
D = 780 K; * = 0.0
Whoops!
Unphysically “negative”  !
Convergence issues?
Symmetry issues?
“Needs more work ;-)”

## Slide 12: OK...Now What About CuO? Well?
Assume a doping density for“g = 0.15 holes/CuO” in this region for experimentally determined Tet-CuO that effectively screens “U” such that we have an “ideal” Fermi liquid.
Then what does Gibbs2 and Eliashberg-McMillan tell us about the possibility of electron-phonon mediated superconducting copper oxide perovskites?

## Slide 13
CuO
(tetragonal)
q = 0.15/CuO
TC
D = 928 K
TC(avg) ~ 75 K
* = 0.05
with maybe a little help from their spins!
Ipso Facto...
At least at optimum doping...
the holes are paired by lattice shakes...

## Slide 14: So What Else is New?
Macfarlane, Rosen, Seki, SSC 63, 831 (1987)
Raman Spectroscopy of YBCO
We can see Phonons have been there ever since the
Creation!

## Slide 15: At the End of the Day... Can We Actually Make Any of this Stuff?

## Slide 16: Aluminum (Quantum-ESPESSO Example)
* = 0.1
Log_w ~ D
TC(exp) = 1.2 K
