## Slide 2
Does the Hold the Key to Room Temperature Superconductivity?
Paul Michael Grant
APS & IOP Senior Life Fellow
IBM Research Staff Member/Manager Emeritus
EPRI Science Fellow (Retired)
Principal, W2AGZ Technologies www.w2agz.com
Room 209, Argyros Forum, 9 May 2017, 9:45 AM – 10:30 AM
Superconducting Fluctuations in One-Dimensional Quasi-periodic Metallic Chains
- The Little Model of RTS Embodied -
8 – 9 May 2017
SUPERHYDRIDES
&
MORE
Aging IBM Pensioner
(research supported under the IBM retirement fund)

## Slide 3: My Three Career Heroes “Men for All Seasons”
“VL”
“Bill”
“Ted”

## Slide 4
May, 2028
(still have some time!)
50th Anniversary of Physics Today, May 1998
http://www.w2agz.com/Publications/Popular%20Science/Bio-Inspired%20Superconductivity,%20Physics%20Today%2051,%2017%20%281998%29.pdf

## Slide 5: “Bardeen-Cooper-Schrieffer”
Where
= Debye Temperature (~ 275 K)
= Electron-Phonon Coupling (~ 0.28)
* = Electron-Electron Repulsion (~ 0.1)
a = “Gap Parameter, ~ 1-3”
Tc = Critical Temperature ( 9.5 K “Nb”)

## Slide 6: Electron-Phonon Coupling a la Migdal-Eliashberg-McMillan (plus Allen & Dynes)
First compute this via DFT…
Then this…
Quantum-Espresso (Democritos-ISSA-CNR)
http://www.pwscf.org Grazie!
Notes: 6

## Slide 7: “3-D”Aluminum,TC = 1.15 K
“Irrational”

## Slide 8
“Put-on !”
Fermion-Boson Interactions
Phonons:
(Al) ~ 430K ~ 0.04eV
Excitons:
(GaAs) ~ 1eV ~ 12,000K
WOW!
Notes: 8

## Slide 9: NanoConcept
What novel atomic/molecular arrangement might give rise to higher temperature superconductivity >> 165 K?

## Slide 10: Little, 1963
Diethyl-cyanine iodide
+
+
+
+
+
+
-
-
-
-
-
-
1D metallic chains are inherently unstable to dimerization and gapping of the Fermi surface, e.g., (CH)x. Ipso facto, no “1D” metals can exist!

## Slide 11: NanoBlueprint
Model its expected physical properties using Density Functional Theory.
  DFT is a widely used tool in the pharmaceutical, semiconductor, metallurgical and chemical industries.
  Gives very reliable results for ground state properties for a wide variety of materials, including strongly correlated, and the low lying quasiparticle spectrum for many as well.
This approach opens a new method for the prediction and discovery of novel materials through numerical analysis of “proxy structures.”

## Slide 12: Fibonacci Chains
“Monte-Carlo Simulation of Fermions on Quasiperiodic Chains,”
P. M. Grant, BAPS March Meeting (1992, Indianapolis)

## Slide 13: A Fibonacci fcc “Dislocation Line”
tan  = 1/ ;  = (1 + 5)/2 = 1.618… ;  = 31.717…°
STO ?
SRO !
Al
Al
Al
Al
Al
Al
Al
L = 4.058 Å (fcc edge) s = 2.869 Å (fcc diag)
...or maybe Na on Si?...in other words...”a proxy Little model!”

## Slide 14: 64 = 65

## Slide 15: “Not So Famous Danish Kid Brother”
Harald Bohr
Silver Medal, Danish Football Team, 1908 Olympic Games

## Slide 16: Almost Periodic Functions
“Electronic Structure of Disordered Solids and Almost Periodic Functions,”
P. M. Grant, BAPS 18, 333 (1973, San Diego)

## Slide 17: APF “Band Structure”
“Electronic Structure of Disordered Solids and Almost Periodic Functions,”
P. M. Grant, BAPS 18, 333 (1973, San Diego)

## Slide 18: Doubly Periodic Al Chain (a = 4.058 Å [fcc edge], b = c = 3×a)
a
Notes: Run 03-11-10_3
Al_Chain_02
Simple Linear Al 1D Chain
Double cell with atoms equally spaced along Al fcc edge = 4.058 Ang, b,c = 3*a, a* = 2*4.058 = 8.116 Ang
Machine 6200 QE e-4.0 Fibo G 6 nat 2 a (au,Ang) 15.34 8.12 a2 (au,Ang) 7.67 4.06 a3 (au,Ang) b (au,Ang) 23.01 12.18 c (au,Ang) 23.01 12.18 ecutwfc(ry) 19 MP-Mesh 16 SCF Time 31m 8.89s NSCF Time 1h47m GSE(ry) -7.89 Ef(eV) -2.92

## Slide 19
Doubly Periodic Al Chain
(a = 2.869 Å [fcc diag], b = c = 6×a)
a
Notes: Run 03-11-10_2
Al_Chain_01
Simple Linear Al 1D Chain
Double cell with atoms equally spaced along Al fcc diagonal = 2.862 Ang, b,c = 3*a, a = 2*2.862 = 5.724 Ang
Machine 6200 QE e-4.0 Fibo G 6 nat 2 a (au,Ang) 10.82 5.73 a2 (au,Ang) 5.42 2.87 a3 (au,Ang) b (au,Ang) 23.01 12.18 c (au,Ang) 23.01 12.18 ecutwfc(ry) 19 MP-Mesh 16 SCF Time 1h 1m NSCF Time 3h 3m GSE(ry) -8.02 Ef(eV) -3.42

## Slide 20
Quasi-Periodic Al Chain
Fibo G = 6: s = 2.868 Å, L = 4.058 Å
(a = s+L+s+s = 12.66 Å, b = c ≈ 3×a)
s
s
s
L
Notes: Run 03-12-10_2
Al_Fibo_05
Gen 6 Fibonacci Chain Selections
Three Al atoms based on fcc distances...b, c scaled to 3 * a0 (4.058)
Machine 6200 QE e-4.0 Fibo G 6 nat 4 a (au,Ang) 23.93 12.66 a2 (au,Ang) 5.42 2.87 a3 (au,Ang) 13.09 6.93 a4 (au,Ang) 18.51 9.79 b (au,Ang) 23.01 12.18 c (au,Ang) 23.01 12.18 ecutwfc(ry) 19 MP-Mesh 16 SCF Time 2h48m NSCF Time 6h32m GSE(ry) -15.99 Ef(eV) -3.20

## Slide 21: Preliminary Conclusions
1D Quasi-periodicity can defend a linear metallic state against CDW/SDW instabilities (or at least yield an semiconductor with extremely small gaps)
Decoration of appropriate surface bi-crystal grain boundaries or dislocation lines with appropriate odd-electron elements could provide such an embodiment.

## Slide 22: What’s Next (1) - Do a Better Job Computationally -
We now have computational tools (DFT and its derivatives) to calculate to high precision the ground and low level exited states of very complex “proxy” structures.
In addition, great progress has been made over the past two decades on the formalism of “response functions,” e.g., generalized dielectric “constant” models.
It should now be possible to “marry” these two developments to predict material conditions necessary to produce “room temperature superconductivity.
A possible PhD thesis project?

## Slide 23: Davis – Gutfreund – Little (1975)

## Slide 26: What’s Next (2) - Build It! -
Today we have lots of tools...MBE (whatever), “printing,” bio-growth...
So, let’s do it!

## Slide 27: NanoConstruction
“Eigler Derricks”
Notes: 27

## Slide 28
h
h

## Slide 29: Fast Forward: 2028

## Slide 30: “You can’t always get what you want…”

## Slide 31: “…you get what you need!”